## Slide 1: The impact of geometric non-linearities on the fatigue analysis of trailing edge bond lines in wind turbine rotor blades
Pablo Noever Castelos, M.Sc.
Andree Stephan, 2007

## Slide 2: Motivation
Source: www.energy.siemens.com; 08.09.2016
Source: www.wind-watch.org; 08.09.2016

## Slide 3: Motivation
High flexibility of modern wind turbine blades Large structural deformations Geometrically non-linear effects | <≠> | 
 |  | Linear superposition principle for the evaluation of fatigue stress histories

## Slide 4: Content
Finite element model and load application
Superposition principle in fatigue analysis
Alternative load application
Conclusion & Outlook

## Slide 5: Content
Finite element model and load application
Superposition principle in fatigue analysis
Alternative load application
Conclusion & Outlook

## Slide 6: Finite element model
  Reference blade: IWES IWT-7.5-164 wind turbine

## Slide 7: Load application
  Approximation of bending moments with concentrated forces
Source: Fraunhofer IWES

## Slide 8: Content
Finite element model and load application
Superposition principle in fatigue analysis
Alternative load application
Conclusion & Outlook

## Slide 9: Superposition principle in fatigue analysis
Load history on blade
Superposition
Linear behaviour is a requirement
Individual loads
Individual responses
Total stress history

## Slide 10: Geometrically non-linear vs. linear analysis
 Linear superposition principle theoretically not applicable!
Shear Stress (GL 2010)
(b) Drucker-Prager equivalent stress
(DNV-GL 2015)

## Slide 11: Content
FE-model and load application
Superposition principle in fatigue analysis
Alternative load application
Conclusion & Outlook

## Slide 12: Alternative load application
  Direct application of internal forces and moments
  All loads can be applied
  Just a small analysis region, repetition necessary

## Slide 13: Geometrically non-linear vs. linear analysis Only bending moments
Shear Stress (GL 2010)
(b) Drucker-Prager equivalent stress
(DNV-GL 2015)

## Slide 14: Geometrically non-linear vs. linear analysis All internal forces and moments
Shear Stress (GL 2010)
(b) Drucker-Prager equivalent stress
(DNV-GL 2015)

## Slide 15: Content
Finite element model and load application
Superposition principle in fatigue analysis
Alternative load application
Conclusion & Outlook

## Slide 16: Conclusion
Geometric non-linearities appear within fatigue load history in 3D FE-analysis
Non-linearities important to be captured for a save blade design
  Impact of non-linearities less severe in multi-axial stress proof
Alternative load application can help to reduce geometric non-linearities

## Slide 17: Outlook
  Evaluation of the non-linearities’ relevance with respect to fatigue life
  Validate geometric non-linearities in real blade tests
  Develop and evaluate new load application strategies for FE analysis

## Slide 18: Contact details
Pablo Noever Castelos, M. Sc.
Institute for Wind Energy Systems
Leibniz Universität Hannover
Appelstraße 9A
D-30167 Hannover, Germany
Phone: +49 511 762 14415
Fax: +49 511 762 4379
E-mail: pablo.noever@iwes.uni-hannover.de